## Slide 1: ULTRASONIC PEENING SOLUTIONS FIELD TRIAL REPORT

## Slide 2: INTRODUCTION
MRA INTERNATIONAL SDN BHD were requested to conduct a field trial on the pipe spool using Ultrasonic Peening Solutions.
Field trial were divided into two types:
  Introduction of external strain on pipe spool
  Removal of external strain on pipe spool.
The field trial were conducted based on capability :
  MMM Stress Measurement Technology
  Ultrasonic Peening Technology

## Slide 3: OBJECTIVES
The objectives of the field trial are:
To determine stress concentration zones (SCZs) area using MMM technology
To implement ultrasonic peening impact on the selected most critical SCZs findings
To determine the correlation between reduction of SCZs based on introduction of external strain and removal of external strain

## Slide 4: METHODOLOGY
Stress Measurement
Ultrasonic Peening Technology
Report Preparation

## Slide 5: IDENTIFICATION OF SCZs LOCATION
External strain due to bolting
Removal of external strain due to bolting

## Slide 6: PERCENTAGE OF REDUCTION FOR MAXIMAL STRESS VALUE
Chart: UPS Treatment
| 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 14
Maximum MMM Stress Level
Percentage Reduction (%) | 1 | 0.65854 | 0.70732 | 0.50146 | 0.44634 | 0.44244 | 0.40146 | 0.42195 | 0.4278 | 0.37122 | 0.36244 | 0.24049 | 0.27073 | 0.26488 | 0.23122
-External strain
-With coating
-Removal external strain
-Without coating
-External strain
-Without coating
Initial (%)

## Slide 7: INITIAL POINT WITHOUT UPS TREATMENT

## Slide 8: 1ST UPS TREATMENT

## Slide 9: 4TH UPS TREATMENT

## Slide 10: CONCLUSION
From the field trial it, it be conclude that:
MMM technology capable in detecting stress occur on the pipe spool
Ultrasonic peening solution capable to reduce the maximum stress occur in selected location
Reduction of stress value is significant with removal of external strain and coating removal.

## Slide 11
Provides various solutions of asset integrity assessment
utilising the capability of latest NDE technology and current inspection approach in obtaining the data gathering for integrity assessment purposes.