Residual Stress

Industrial Applications

Many structural weldments – ships, offshore platforms, cranes, bridges, large reservoirs, large metallic constructions, machinery, antennas, and other structures are subjected to the action of a large number of cyclic loads during service. The development of fatigue fractures amounts to approximately 30% of the total premature failures in these structures.

The fatigue limit of butt welds in different strength classes of steel established by the criterion of fatigue crack initiation is reduced to between 32% and 46% of the fatigue limit of corresponding parent metal with a rolled surface. Similarly, the fatigue limit of lap joints with longitudinal fillet welds under cyclic stress conditions constitutes only 20% to 40 % of the fatigue limit of the corresponding parent metal.

What is Residual Stress?

Residual stresses are present in many fabricated structures due to local plastic deformation from thermal and mechanical operations during the manufacturing or use. The presence of residual stresses in engineering components and structures can significantly affect the fatigue behaviour during external cyclic loading.

The effect of residual stresses may either be beneficial or detrimental, depending on magnitude, sign (compressive or tensile) and distribution of the stresses with respect to the load-induced stresses. Residual stresses in tension are detrimental and are often in the magnitude of the materials yield strength. These tensile residual stresses will reduce the fatigue life of the structure by increasing the growth of the fatigue crack. In comparison, compressive residual stresses will decrease fatigue crack growth rate.

What causes Residual Stress?

Residual stresses can occur through a variety of mechanisms including inelastic (plastic) deformations, temperature gradients (during thermal cycles) or structural changes (phase transformation).

Cold working, hot rolling, grinding, quenching treatments, welding, and thermal cutting can all induce residual stress into metal. The nature of residual stress, its distribution, and prediction of the level within a metal is a complex and not completely understood phenomenon, but you can be sure it is present.

Welding, in particular, because of the rapid thermal expansion and contraction created along a very localized area, is a prime source of residual stress. A very high heat source is applied to a small area relative to the cooler surrounding area. That point where the arc is directed is rapidly heated from ambient temperature to temperatures that can be in excess of 1,600°C. The metal expands as it is brought to a molten state. As the molten weld pool solidifies along the joint, there is resistance to its shrinkage by the already solidified weld metal and the solid base metal adjacent to the weld. This resistance creates a tensile strain in the longitudinal and transverse directions of the weld. Distortion is often the result, and if the stress is excessive, buckling, stress corrosion cracking, and shortened fatigue life are possible.

All welds will have some residual stress, and it will never be totally reduced to zero strain. But the level of stress can be very high depending on certain conditions. Heat input, base metal thickness, cooling rate, restraint of the weldment, and welding process play roles in the level of residual stress induced into a weldment.

How is Residual Stress Removed?

There are essentially three approaches to stress relief:

Thermal treatment is the first and this method is currently used in industry by means of heating ovens. This approach is used mainly for smaller parts also with large series. Treatment costs are relatively high (due mainly to energy requirements) compared to other mechanical stress relief methods. Larger parts (several meters in diameter) cannot feasibly be treated in this manner due to the technical challenges and the high cost aspects (CAPEX and OPEX).

Shot peening is a cold working method that reduces stress. Small, round metal balls, or shot, are projected onto the surface of the weldment. The shot imparts small indentations into the surface, which induces compressive stress. The tensile residual stresses at the surface of the weldment must "overcome" the compressive stress for a fatigue crack to initiate. If properly applied, the compression works to counteract the tensile stresses. Fatigue cracks have a low probability of developing in the shot-peened area.

Vibratory Stress Relief is another mechanical means of stress relief is by vibration. A mechanical vibrating device is attached to the weldment. The vibration's resonant frequency can be controlled by specially designed machines. The amount of time the weldment is subjected to the vibration is usually dependent on its weight. The vibration can be applied during or immediately after welding. The vibration seems to even the stress distribution within the weldment by means of plastic deformation of the metal's grains, reducing sharp peaks of stress.

The MPI Ultrasonic Peening Technology.

The MPI Ultrasonic Peening is an advanced technology that modifies the physical and metallurgical properties of a component. While some fatigue life improvement techniques relies on the change of the geometrical shape of the weld toe (grinding, TIG dressing, etc), others relies on the introduction of compressive residual stresses (hammer peening, spot heating, etc). The MPI Ultrasonic Peening treatment achieves simultaneously the improvement of weld toe geometry and the deep introduction of beneficial compressive residual stresses, during the same work operation.

- Increased Fatigue Resistance

- Increased Corrosion Resistance

- Decreased Residual Deformation

- Decreased Residual Weld Stress

No other stress relief method including Grinding, Shot Peening, Hammer Peening, or  TIG Dressing can achieve all the above results

(Please pay attention on the text “LETS” since owner of LETS could react.  They cannot attack me if I am selling such equipment, but better to modify the pictures coming from LETS).

Why is the MPI Peening Technology Unique (to other peening technologies?)

- Faster

- More effective (penetration)

- Cheaper  (in fact I was selling for 35’000 EUR)

- Longer lasting (average operating life extended for 20 years)

Need such bullets. “High power ultrasonics” is good but doesn’t say a lot! Need clear bullet points please

Comparison of  MPI Peening Vs Post Welded Heat treatment

MPI Process

Reduction of tensile residual stresses via introduction of compressive stress

Improves brittle facture resistance of welded joints.

Improves the toughness of weld metal heat effected zone.

Useful for weld thickness up to 12 mm. For 40 mm thick weld the treatment can be applied after every weld pass.

Easy to apply due to the fact that UP equipment is small and versatile even for difficult access.

Shorter time required for treatment, less energy used during treatment.

Treatment can be applied in situ or in specific areas

Environmentally friendly due to energy saving

Low capital cost

10% hardness increase and 50% surface quality improvement

Reduced rate of micro pitting leading to improved surface fatigue resistance

PWHT Process

Reduction of tensile residual stresses via introduction of compressive stress

Improves brittle facture resistance of welded joints.

Improves the toughness of weld metal and heat effected zone.

Useful for highly stressed nodal welds greater than 40 mm thick and other welds greater than 50 mm thick.

Difficult to apply on welded structures.

Longer time required for treatment, high energy used during treatment.

Difficult to apply in situ or area specific.

High energy use/cost

High capital cost

Modular design of the Peening tool

Easy maintenance and replacements of parts.

Non