## Slide 1: Multifrequency Ultrasonic Treatment as a Liquid-State Processing Method of Aluminum Alloys
Raquel Fierro Jaime1, Andrew Zang1,2, Adrianne Chang1, Miodrag Prokic3, Martijn Vos4, Carl Söderhjelm1,2, Hélder Puga1,5, Diran Apelian1,2
1University of California Irvine, 2Pratt & Whittney Center of Excellence, 3MPI Interconsulting, 4Aluminium Rheinfelden, 5CMEMS, University of Minho, Guimarães, Portugal

## Slide 2
Outline
Ultrasonic Treatment (UST) for Al Recycling
Liquid-State Multifrequency UST
Results
Conclusions
(3 min.)
(5 min.)
(8 min.)
(3 min.)
Total: 20 min.

## Slide 3
Outline
Ultrasonic Treatment (UST) for Al Recycling
Liquid-State Multifrequency UST
Results
Conclusions

## Slide 4
Primary Aluminum
1.2 Billion Tons of CO2 for 80,000 Tons of Al per year
P. McKenna, et. al ICN 2023 S. Padamata, et. al JOM 2021
> 3.8 Million Tons Secondary Aluminum per year
➞ post-consumer scrap available to recover
93% Reduction in CO2
Liquid Metal Processing
β-Al5FeSi
⍺-Al15Fe3Si2
Detrimental Intermetallics
Recovery of Aluminum Alloys

## Slide 5
➞ Tailor the microstructure via grain size & intermetallic morphology
Traditionally: Chemical additives
Liquid Metal Processing
Degassing
Grain Refinement
Intermetallic Morphology Modification
Sustainable approach must be developed
Ultrasonic Treatment (UST)
➞ ‘Metal Cleanliness’: Hydrogen & inclusion removal
Processing for Secondary Aluminum Recovery
Traditional methods: Rotary Degassing, Chemical Flux

## Slide 6
Outline
Ultrasonic Treatment (UST) for Al Recycling
Liquid-State Multifrequency UST
Results
Conclusions

## Slide 7
UST Processing of Molten Metal
Application of ultrasonic energy into molten metal for microstructural modification
Ultrasonic Frequency
= 18-22 kHz
UST Probe
Liquid Metal
Acoustic Cavitation
Acoustic Streaming
Expansion ~10 MPa
5000°C
5000m/s
D. Eskin, et. al 2014

## Slide 8
UST Processing of Molten Metal
Application of ultrasonic energy into molten metal for microstructural modification
UST Probe
Liquid Metal
Acoustic Cavitation
Acoustic Streaming
Unproven
Grain Refinement & Intermetallic Modification

## Slide 9
Multifrequency Multimode Modulated (MMM)
Fixed Frequency
Frequency Delivery in UST Systems
Accounts for multiple external frequencies
System Adaptive Processing
Most common in the field
Does not counteract decay
Gradient of treatment
Source
Sensor

## Slide 10
Photo Courtesy H. Puga
Waveguide
Hollow SiAlON Probe
PZT Transducer
Clamp
720, 700, 680, 660 °C
5, 10, 15 minutes
5, 10, 20 kilograms
5, 10, 20 min. post-UST
Mass Treated
Treatment Time
Treatment Temperature
Decay with Time
Multifrequency UST Experiments

## Slide 11
Outline
Ultrasonic Treatment (UST) for Al Recycling
Liquid-State Multifrequency UST
Results
Conclusions

## Slide 12
⍺-Al15Fe2Si3
Eutectic Si
Al2Cu
Primary Al
1
2
3
4
10 µm
As-Cast Aluminum A380
A380 | 
 | wt. %
Si | 8.25
Cu | 3.53
Zn | 2.27
Fe | 0.845
Mn | 0.200
Cr | 0.070
P | 0.001
A380 TL=585°C

## Slide 13
UST Grain Refinement of A380
11% Decrease
86% Decrease
77% Decrease
What is the underlying mechanism of UST Grain Refinement?
Treatment Temperature
A380 TL=585°C
Connection between Grain Size & Intermetallics

## Slide 14
Primary Si
Polyhedral Fe
Si-Phase at all Temps
Fe-Phase only ≦ UST at 680°C
A380 TL=585°C
Treatment Temperature
Intermetallic Modification

## Slide 15
Primary Si
Xu, et al J. Crys. Gr. 2006
Serial Sectioning to Reveal Potential Nucleus
Collaboration with Dr. A. Zang
Al-18Si
J. Li et. al Nat. Sci. R. 2016

## Slide 16
Thermal Analysis
Primary Al
⍺-Al15(Fe, Mn)3Si2
Eutectic Si
Al₂Cu
Untreated A380

## Slide 17
Thermal Analysis
Primary Al
⍺-Al15(Fe, Mn)3Si2
Eutectic Si
Al₂Cu
No-UST 700°C
UST 700°C
UST 700°C
UST 680°C
UST 660°C
Primary Al
Polyhedral Fe seen in samples with 2 peaks
⍺-script
Undercooling
Reduction in undercooling
Primary Si undetectable during early stages of solidification
Indicators of Primary Solidification:
Nucleation Pathway
‘Survives Remelting’

## Slide 18
Grain Size: Treatment Time
5
As-Cast
15
Treatment Time
OM EBSD
β-AlFeSi
After Al
⍺-AlFeSi
After Al
⍺-AlFeSi
After Al
Treatment Time (min)
10
Average Grain Size (µm)
Grain Size ↓ with ↑ UST Time
700°C
Expected for Refinement via Oxides

## Slide 19
Grain Size: Treatment Time
EBSD
β-AlFeSi
After Al
Polyhedral-Fe
Before Al
660°C
OM
5
As-Cast
15
Treatment Time (min)
Average Grain Size (µm)
10
Grain Size Oscillates with Fe-Phase Morphology
Polyhedral-Fe
Before Al
Intermetallic Morphology influences Grain Refinement
Treatment Time

## Slide 20
Outline
Ultrasonic Treatment (UST) for Al Recycling
Liquid-State Multifrequency UST
Results
Conclusions

## Slide 21
In Addition to Refinement via Oxides:
UST alters Solidification Chronology
Chronology influences Morphology
Morphology influences Grain Refinement
Conclusions

## Slide 22
Thank you!
Special Thanks to Prof. Hélder Puga, Dr. Andrew Zang, and Adrianne Chang
Contact: Raquel Fierro Jaime
rfjaime@uci.edu
Acknowledgements

## Slide 23
About the Presenter
Raquel Fierro Jaime
Doctoral Candidate
Advanced Casting Research Center
University of California, Irvine
Highest Degree
M.S. Materials Science & Engineering 2025
University of California, Irvine
Undergraduate Degree
B.S. Materials Science & Engineering 2022
University of California, Riverside
Research Interests
Metallurgy, Metal Casting, Aluminum, Sustainability, High Entropy Alloys, Material Processing, Solidification
Questions? ➞ rfjaime@uci.edu
Notes: Enter speaker notes here.