## Slide 1: Ultrasonic vibrations in metallurgy… with MMM Technology
Degassing of Al and Mg alloys
Grain refinement of Al and Mg alloys
www.UltrasonicMetallurgy.com
MP Interconsulting Marais 36, 2400 Le Locle, Switzerland
www.UltrasonicsWorldGroup.com
Phone: +41-32-9314045
Fax: +41-32-9314079
www.mpi-ultrasonics.com
mpi@mpi-ultrasonics.com
by M. Prokic
Patent
European Patent Application (related to MMM technology): EP 1 238 715 A1
Multifrequency ultrasonic structural actuator
Applicant: Prokic Miodrag, MP Interconsulting, 5.03.2001 – 11.09.2002

## Slide 2
2021 ® MP Interconsulting || Marais 36, 2400 Le Locle, Switzerland ||www.UltrasonicsWorldGroup.com || mpi@mpi-ultrasonics.com
… proposal for your factory:
Cavitation in Metallurgy
Degassing
Principle:
Supplying acoustic energy to a melt, in order to induce cavitation and initiate Sonocrystallization:
(i) A great number of small cavities developed inside the liquid.
(ii) Diffusion of hydrogen from the melt to developed bubbles
(iii) Large bubbles coagulate and float to a surface of liquid pool
Refinement of
a-Al
Besides degassing, the development of cavitation promotes significant undercooling and formation of numerous solidification nuclei.
Grain refinement exerts a positive influence on several properties of cast aluminum, namely: porosity, shrinkage distribution, intermetallic distribution and mechanical properties.
Ultrasound above the threshold of acoustic cavitation can be introduced into a molten metal promoting:
Degassing of liquid metals using high intensity ultrasonic activity.
Grain refinement, Si eutectic and intermetallic modification.

## Slide 3
2021 ® MP Interconsulting || Marais 36, 2400 Le Locle, Switzerland ||www.UltrasonicsWorldGroup.com || mpi@mpi-ultrasonics.com
… proposal for your factory:
Cavitation in Metallurgy
Degassing

## Slide 4
2021 ® MP Interconsulting || Marais 36, 2400 Le Locle, Switzerland ||www.UltrasonicsWorldGroup.com || mpi@mpi-ultrasonics.com
MPI Dedicated Software Control

## Slide 5
2021 ® MP Interconsulting || Marais 36, 2400 Le Locle, Switzerland ||www.UltrasonicsWorldGroup.com || mpi@mpi-ultrasonics.com
… New Device for You
Dynamic Stirring rotation
available for degassing of aluminum alloys in a furnace / crucible

## Slide 6
2021 ® MP Interconsulting || Marais 36, 2400 Le Locle, Switzerland ||www.UltrasonicsWorldGroup.com || mpi@mpi-ultrasonics.com
Degassing
Refining
Modification
a-Al
Si
Intermetallics
Porosity
Al-Si-Cu
0 min
1 min
3 min
5 min
Spatial distribution of acoustic flow from the transducer radial sonication of SiAlON tube.

## Slide 7
2021 ® MP Interconsulting || Marais 36, 2400 Le Locle, Switzerland ||www.UltrasonicsWorldGroup.com || mpi@mpi-ultrasonics.com
The samples with ultrasonically treated melt display a moderate grain refinement. The micrographs can evidence this behavior, as the Argon degassed micrograph in Figure (a) displays large dendrites, while Figures (b) and (c) show globular and rosette-like α-Al grains, highlighting some moderate grain refinement promoted by the ultrasonic melt treatment.
Degassing
Refining
Modification
a-Al
Si
Intermetallics
Porosity
(a)
(c)
(b)

## Slide 8
2021 ® MP Interconsulting || Marais 36, 2400 Le Locle, Switzerland ||www.UltrasonicsWorldGroup.com || mpi@mpi-ultrasonics.com
Al-Si-Cu after ultrasonic processing
Al-Si-Cu before ultrasonic processing
Optical microscope (OM) and Scanning Electron Microscope (SEM) with quantitative metallographic analysis capability were used to evaluate the shape and grain size of constituents ….
Degassing
Refining
Modification
a-Al
Si
Intermetallics
Porosity

## Slide 9
2021 ® MP Interconsulting || Marais 36, 2400 Le Locle, Switzerland ||www.UltrasonicsWorldGroup.com || mpi@mpi-ultrasonics.com
Optical microscope (OM) and Scanning Electron Microscope (SEM) with quantitative metallographic analysis capability were used to evaluate the shape and grain size of constituents ….
Degassing
Refining
Modification
a-Al
Si
Intermetallics
Porosity

## Slide 10
2021 ® MP Interconsulting || Marais 36, 2400 Le Locle, Switzerland ||www.UltrasonicsWorldGroup.com || mpi@mpi-ultrasonics.com
… proposal for HPDC …
Cavitation in Metallurgy
Degassing
available for degassing and refinement localized of aluminum alloys in a HPDC process
… new concept …
… adjustable …

## Slide 11
2021 ® MP Interconsulting || Marais 36, 2400 Le Locle, Switzerland ||www.UltrasonicsWorldGroup.com || mpi@mpi-ultrasonics.com
… proposal for HPDC …
Cavitation in Metallurgy
Degassing
available for degassing and refinement localized of aluminum alloys in a HPDC process
… new concept …
… adjustable …

## Slide 12: Thank You.
www.UltrasonicMetallurgy.com
MP Interconsulting Marais 36, 2400 Le Locle, Switzerland
www.UltrasonicsWorldGroup.com
Phone: +41-32-9314045
Fax: +41-32-9314079
www.mpi-ultrasonics.com
mpi@mpi-ultrasonics.com
… the future of your company start here with MMM Technology.