## Slide 1: Innovative High Drive Piezoelectric Ceramic for Use in High Power Transducers Piezotech, LLC
De Liufu, Jared Brosch, Andreas Hadjicostis, William Shelley, Michael Phillips, Craig Miller
Notes: Piezotech, LLC

## Slide 2: Introduction
Development a new high drive piezoelectric ceramic
Testing new material’s performance by construction and testing of transducers
Comparison against other commercially available high drive PZT

## Slide 3: Introduction
Acoustic Power P=2  frE²k²εT33Qm
A PZT-based high power piezoceramic formula was developed with the material performance as follows:
Material Type | Qm | T33 | kp | Qm * T33 * kp
Navy Type I | 500 | 1275 | 0.58 | 370 x 103
Navy Type III | 800 | 1025 | 0.50 | 410 x 103
Piezotech New | 1000 | 3000 | 0.55 | 1650 x 103
Property | Dielectric Constant | Qm | kp | d33 (pC/N) | tan  | Density (g/cm3) | Tc (oC) | Grain Size (m)
Nominal Value | 2700 | 1000 | 0.55 | 375 | 0.006 | 7.7 | 215 | 3 to 5

## Slide 4: Dielectric Characteristics

## Slide 5: Ceramic Microstructure
Fine, uniform grain size
Evidence of trans-granular fracture
Few, small pores

## Slide 6: DC De-Poling Performance at Room Temperature.

## Slide 7: Accelerated Aging Characteristics at 130ºC

## Slide 8: Accelerated Aging Characteristics at 130ºC

## Slide 9: Transducer Testing
Two transducer models were tested using the new material.
  A high power device at 40Khz (Etalon QI-40), used typically for ultrasonic cleaning and sieve shaking
  A high power single element transducer at 1.5Mhz, could be used in industrial or medical industries
Both transducer models were built using Keramos K-270 (Navy Type I equivalent) and the new material.

## Slide 10
Etalon Standard QI-40 40Khz Cleaning/Shaking device shown with some example horns.
10mm 1.5Mhz Air backed transducers
Built for Total Acoustic Power measurements
Similar transducers may be applicable in both medical and industrial settings

## Slide 11
433Ohms, - 51deg. Coupled into Water.
Frequency marker chosen at peak Conductance
QI-40 with K-270

## Slide 12
170Ohms, - 7deg. Coupled into Water.
Frequency marker chosen at peak Conductance
QI-40 with New Material

## Slide 13: Output Power Measurement
The QI-40 units were placed under power, and their output was observed while attached to screens and in water. Both units seemed to perform identically.
Further testing on a laser vibrometer will be done to look at the output displacement versus input power.
Other methods for power output measurement will attempted as well.

## Slide 14
97 Ohms, - 20 deg. Coupled into Water
Frequency marker chosen at peak Conductance
1.5 Mhz with K-270

## Slide 15
53 Ohms, - 21 deg. Coupled into Water
Frequency marker chosen at peak Conductance
1.5 Mhz with New Material

## Slide 16: TAP Testing Experimental Setup
Frequency of operation was set at peak conductance using an SRS DS345 function generator with a continuous sine wave.
The units were powered with an ENI2100L 50 ohm output amplifier
Total Acoustic Power was recorded with a UPM-DT-1 ultrasound power meter in water.
Input power was recorded with an HP54645A oscilloscope with voltage and current probes

## Slide 17
Linear relationship as expected
Approximately 43% efficient

## Slide 18
Linear relationship similar to K-270
Approximately 45% efficient

## Slide 19: Conclusions
A new material is being developed that improves on current Navy I equivalent materials.
The new material has equal or better performance in the tested high power transducers.
The impedance of the transducers with new material shows a 50% or greater reduction. This allows for possible better matching to source impedances and improved electrical efficiency.
Higher d33 value should allow for higher displacement at high power.
This ceramic may be applicable for high power composites and therapeutic array work, as well as industrial high power applications.